INSPECTION APPROVAL NOTE

| Ref no | INSP-2026-003 |
| --- | --- |
| Date | 26-09-2026 |
| Subject | Annual Inspection Report for Tank T-104 |

# Background

Tank T-104 was taken out of service on 08-09-2026 for annual inspection. The last inspection in September 2025 reported general corrosion within limits.

# Findings

| S.No | Item | Observation | Severity | Source page |
| --- | --- | --- | --- | --- |
| 1 | Shell course 2, north side | Wall thinning to 6.1 mm against 8.0 mm nominal (24% loss). Below 80% of nominal thickness. | High | 1 |
| 2 | Bottom plate near sump | Pitting up to 1.2 mm deep. | Medium | 1 |
| 3 | Confined space entry permit | No spade blind fitted on N2 during entry; no gas test entries on the permit after 11:00; attendant left the manway for about 10 minutes. | High | 1 |
| 4 | Inlet nozzle N2 and mixer MX-104 | Mixer motor breaker was switched off but not locked or tagged. | Medium | 1 |
| 5 | Roof handrail and stairway | Surface rust and coating breakdown. No loss of section. | Low | 1 |

# SOP references

| S.No | Document | Page |
| --- | --- | --- |
| - | Not applicable | - |

# Recommendation

Replace the thinned plates before returning the tank to service, ensuring welding is done under a hot work permit after cleaning and gas testing. Fit a spade blind on nozzle N2 and apply lockout/tagout to the mixer motor.

# Cost implication

To be filled by the originator.

# Approval

|  | Prepared by | Reviewed by | Approved by |
| --- | --- | --- | --- |
| Name | M. P. Joshi |  |  |
| Designation |  |  |  |
| Signature |  |  |  |
| Date |  |  |  |